# Multi-layer woven synthetic fabrics

Мaterial: polyester  monofilament (PET)

Polyamide monofilament (РА 6; РА 6,6)

| Fabric number, type of weave and longitudinal section along warp yarns | Maximum cloth’s width, mm | Nominal yarns diameter, mm |  |  | Number of yarns per 1 running centimeter of fabric, pcs |  |  | Air permeability, CFM | Elongation of fabric long warp yarns at 10 kg/cm load, %, not more than | Cloth’s thickness, mm | Nominal weight of 1 m2 of cloth, kg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | warp | Upper weft | Lower weft | warp | weft |  |  |  |  |  |
| 2- layer fabrics with heatsetting |  |  |  |  |  |  |  |  |  |  |  |
| 7-shaft fabrics |  |  |  |  |  |  |  |  |  |  |  |
| 37 · · · · · · · · · · · · · · | 7000 | 0.30 | 0,30 | 0,32 | 37 | 22-24 |  | 262-410 | 0,7 | 1,00-1,20 | 0,724 |
| 37 · · · · · · · · · · · · · · | 7000 | 0,30 | 0,30 | 0,32 0,34PA | 37 | 22-24 |  | 361-459 | 0,7 | 1,00-1,25 | 0,741 |
| 40 · · · · · · · · · · · · · · | 9200 | 0.17 | 0,18 | 0,20 0,20 PA | 40 | 58-62 |  | 230-361 | 1,3 | 0,62-0,69 | 0,409 |
| 40 · · · · · · · · · · · · · · | 9200 | 0,17 | 0,20 | 0,27 0,28PA | 40 | 35,5 -36,5 |  | 525-607 | 1,3 | 0,75-0,80 | 0,403 |
| 47 · · · · · · · · · · · · · · | 9200 | 0.25 | 0,25 | 0,27 | 47 | 24-26 |  | 312-443 | 0,8 | 0,90-0,94 | 0,599 |
| 55 · · · · · · · · · · · · · · | 9200 | 0.20 | 0,20 | 0,22 0,22PA | 55 | 34-36 |  | 312-410 | 1,0 | 0,73-0,77 | 0,470 |
| 8-shaft fabrics |  |  |  |  |  |  |  |  |  |  |  |
| 22 · · · · · · · · · · · · · · · · | 7000 | 0,45 | 0,45 0,50 | 0,50 | 22 |  | 17-19 | 410-574 | 0,6 | 1,65-1,81 | 1,102-1,156 |
| 24 · · · · · · · · · · · · · · · · | 7000 | 0,25 | 0,30 | 0,32 0,34PA | 24 |  | 36-38 | 394-492 | 0,9 | 1,10-1,12 | 0,627 |
| 60 · · · · · · · · · · · · · · · · | 9200 | 0,17 | 0,20 | 0,22 0,22PA | 60 |  | 44-46 | 197-328 | 1,0 | 0,68-0,70 | 0,458 |
| 60 · · · · · · · · · · · · · · · · | 9200 | 0,17 | 0,18 | 0,20 0,22PA | 60 |  | 44-46 | 230-328 | 1,0 | 0,65-0,70 | 0,437 |
| 2,5-layer fabrics (with supporting weft yarns) with heatsetting |  |  |  |  |  |  |  |  |  |  |  |
| 37 8-shaft fabric • • • • • • • • • • • • • • • • • • • • • • • • |  | 0.27 | Uı –0.20 U2 –0.24 | L-0.45 | 37 | Uı-11.5 U2 11.5 L-11.5 |  | 394-459 | 0,7 | 1,18-1,21 | 0,788 |
| 60 16-shaft fabric • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • • 0,17 Uı –0.13 U2 –0.17 |  |  |  | Lı –0.27 L2 –0.28PA | 60 | Uı – 19 U2 – 19 Lı –9,5 L2 –9,5 |  | 328-394 | 1,0 | 0,75-0,77 | 0,497 |
| 3-layer fabrics with heatsetting |  |  |  |  |  |  |  |  |  |  |  |
| 60 20-shaft fabric |  | U-0.13 L-0.17 | Uı –0.13 U2 –0.15 | Lı –0.30 L2 –0.30PA | 30.0 30.0 | Uı – 34 U2 – 17 Lı – 8,5 L2 – 8,5 |  | 279-344 | 1,0 | 1,65-1,80 | 0,484 |

NOTE:

1. Fabric number indicates nominal number of warp yarns per running centimeter.

2. In double layer fabrics warp and weft yarns in the upper layer are made of polyester monofilament; in the lower layer polyester and polyamide monofilaments are 1:1. If agreed upon by the supplier and the consumer weft yarns of the lower layer are made of polyester monofilament.

3. Fabrics are produced as a seamed (endless) or seamless cloth. In endless cloth the following seams are used:  sewn, loop detachable, spiral or clipper detachable, woven straight.

4. All 2-layer fabrics from 15 to 55 m long are treated on tension machine with heatsetting.

5. Endless 2-layer fabrics No.40 and No.60 from 15 to 55 m long undergo grinding; the rest fabrics (excluding No.22) undergo grinding if agreed upon by the parties.

6. Multilayer fabric’s cost is calculated according to a definite order and depends on the fabric’s size, seaming, heatsetting, grinding, edge treatment.

Physical characteristics of synthetic woven fabrics

| Fabric strength, kg/cm | 52 -180 |
| --- | --- |
| Relative elongation of fabric along warp yarns after heatsetting at 10 kg/cm load, % | 0.6 – 0.7 |
| Temperature of polyester emolliating, °C | +230 – (+249) |
| Fabric working temperature, °C - working temperature of fabrics made of polypropylene | (-40) – (+60) from -15°C to +60°C |

Synthetic fabrics made of polyester monofilament

- are resistant to mineral and organic acids,  alkalis (with concentration not more than 10%, pH 9-11) and organic solvents (acetone, benzene, 4-chloride carbon);

- have  high resistance to atmospheric exposure, are not dissolved in water, have  biochemical resistance, are good electric insulting materials;

- are dissolved in phenols, concentrated sulfuric acid and hydrogen nitrate;

- must not be subject to prolonged exposure of  high temperature steam (above +110°C) because it causes hydrolytic destruction of monofilament and decline in strength;

- synthetic fabrics made of polyester monofilament, containing also polyamide yarns, mustn’t be cleaned with mineral and organic acids as well as chemicals with oxidizing properties (for example, peroxides), because it may lead to polyamide yarns destruction.