# Single warp woven wire mesh

Application: In pulp-and-paper industry for production of different types of paper, cardboard, pulp; for production of asbestos items for construction; in coal, mining, chemical industries, geology and nature protection as filtering materials and transporting devices.

| Mesh № | Nominal wire diameter, mm Wire material warp weft |  |  | Size of opening between, mm warp wires weft wires |  |  | Cross-section area of mesh, % |  | Nominal weight of 1 m2 of cloth, kg |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Warp: tin-phosphor bronze BrОPh 6,5-0,4 (8,0-0,3); Weft: brass 80/20 |  |  |  |  |  |  |  |  |  |  |  |  |  | Warp: tin-phosphor bronze BrОPh 6,5-0,4 (8,0-0,3); Weft: brass 80/20 |  |
| 18 | 0.25 |  | 0.27 | 0.306 |  | 0.444 | 34,21 |  | 1.574 |  |  |  |  |  |  |
| 20 | 0.25 |  | 0.27 | 0.250 |  | 0.397 | 29,75 |  | 1.715 |  |  |  |  |  |  |
| 22 | 0.25 |  | 0.27 | 0.205 |  | 0.397 | 26,78 |  | 1.807 |  |  |  |  |  |  |
| 24 | 0.25 |  | 0.27 | 0.167 |  | 0.397 | 23,80 |  | 1.900 |  |  |  |  |  |  |
| 26 | 0.23 |  | 0.25 | 0.155 |  | 0.356 | 23,62 |  | 1.758 |  |  |  |  |  |  |
| 28 | 0.22 |  | 0.24 | 0.137 |  | 0.366 | 23,19 |  | 1.686 |  |  |  |  |  |  |
| 32 | 0.19 |  | 0.21 | 0.123 |  | 0.331 | 23,97 |  | 1.437 |  |  |  |  |  |  |
| 36 | 0.15 |  | 0.18 | 0.128 |  | 0.246 | 26,54 |  | 1.125 |  |  |  |  |  |  |
| 40 | 0.13 |  | 0.15 | 0.120 |  | 0.242 | 29,64 |  | 0.920 |  |  |  |  |  |  |
| Warp and weft: stainless steel AISI 321, AISI 316 |  |  |  |  |  |  |  |  |  |  |  |  | Warp and weft: stainless steel AISI 304, AISI 321 (AISI 316) |  |  |
| 10 | 0.40 |  | 0.40 | 0,600 |  | 0.776 | 39,60 |  | 2,041 |  |  |  |  |  |  |
| 10 | 0,35 |  | 0,35 | 0,650 |  | 0,826 | 45,66 |  | 1,525 |  |  |  |  |  |  |
| 14 | 0.35 |  | 0.35 | 0,364 |  | 0.,703 | 33,61 |  | 2,000 |  |  |  |  |  |  |
| 16 | 0.25 |  | 0.25 | 0,375 |  | 0,583 | 42,00 |  | 1,189 |  |  |  |  |  |  |
| 16 | 0.25 |  | 0.28 | 0,375 |  | 0.553 | 39,84 |  | 1,313 |  |  |  |  |  |  |
| 16 | 0.25 |  | 0.30 | 0,375 |  | 0.533 | 38,40 |  | 1,403 |  |  |  |  |  |  |
| 16 | 0,28 |  | 0,30 | 0,345 |  | 0,533 | 35,33 |  | 1,582 |  |  |  |  |  |  |
| 18 | 0.25 |  | 0,25 | 0,306 |  | 0.519 | 37,13 |  | 1,306 |  |  |  |  |  |  |
| 18 | 0.25 |  | 0.28 | 0,306 |  | 0.489 | 34,98 |  | 1,440 |  |  |  |  |  |  |
| 22 | 0.20 |  | 0.22 | 0.255 |  | 0.336 | 33,82 |  | 1.177 |  |  |  |  |  |  |
| 24 | 0.20 |  | 0.24 | 0,217 |  | 0.405 | 32,66 |  | 1,248 |  |  |  |  |  |  |
| 32 | 0,18 |  | 0,20 | 0,133 |  | 0,341 | 26,71 |  | 1,198 |  |  |  |  |  |  |
| Fabrics for production of special paper grades |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Warp: tin-phosphor bronze BrOPh 6,5-0,4 (8,0-0,3) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 7 | 0,45 |  | 0,45 BrOPh | 0,979 |  | 0,979 | 46,92 |  | 2,183 |  |  |  |  |  |  |
| 7 | 0,45 |  | 0,50 BrOPh | 0,979 |  | 0,929 | 44,53 |  | 2,436 |  |  |  |  |  |  |
| 9 | 0,35 |  | 0,40 BrOPh | 0,761 |  | 0,600 | 41,10 |  | 2,039 |  |  |  |  |  |  |
| 9 | 0,50 |  | 0,50 BrOPh | 0,611 |  | 0,611 | 30,25 |  | 3,413 |  |  |  |  |  |  |
| 12 | 0,31 |  | 0,31 BrOPh | 0,523 |  | 0,523 | 39,44 |  | 1,735 |  |  |  |  |  |  |
| 14 | 0,26 |  | 0,26 BrOPh | 0,454 |  | 0,454 | 40,45 |  | 1,415 |  |  |  |  |  |  |
| 14 | 0,26 |  | 0,30 BrOPh | 0,454 |  | 0,414 | 36,89 |  | 1,646 |  |  |  |  |  |  |
| 16 | 0,25 |  | 0,28 BrOPh | 0,375 |  | 0,387 | 34,80 |  | 1,620 |  |  |  |  |  |  |
| 16 | 0,25 |  | 0,27 brass 80/20 | 0,375 |  | 0,397 | 35,70 |  | 1,568 |  |  |  |  |  |  |
| 16 | 0,27 | 0,30 brass 80/20 |  | 0,355 | 0,533 |  |  | 36,35 | 1,654 |  |  |  |  |  |  |
| 26 | 0,23 |  | 0,25 brass 80/20 | 0,155 |  | 0,356 | 23,62 |  | 1,758 |  |  |  |  |  |  |
| 28 | 0,21 |  | 0,23 BrOPh | 0,147 |  | 0,296 | 23,19 |  | 1,663 |  |  |  |  |  |  |
| 28 | 0,22 |  | 0,24 brass 80/20 | 0,137 |  | 0,366 | 23,19 |  | 1,686 |  |  |  |  |  |  |
| 32 | 0,18 |  | 0,18 BrOPh | 0,133 |  | 0,237 | 24,08 |  | 1,331 |  |  |  |  |  |  |
| 32 | 0,18 |  | 0,20 BrOPh | 0,133 |  | 0,217 | 22,05 |  | 1,461 |  |  |  |  |  |  |
| 32 | 0,165 |  | 0,18 BrOPh | 0,148 |  | 0,237 | 26,81 |  | 1,201 |  |  |  |  |  |  |
| 32 | 0,165 |  | 0,18 brass 80/20 | 0,148 |  | 0,237 | 26,81 |  | 1,183 |  |  |  |  |  |  |

Note:

1. Mesh number indicates nominal number of warp wires per centimeter.

2. Meshes are produced as a seamed (endless) and seamless cloth. In endless cloths the following seams are used: on mesh made of non-ferrous metals - gas soldered (straight and diagonal), electro-soldered, sewn, loop (detachable) seams are made; on mesh made of stainless steel wire - sewn, loop (detachable), gas soldered (straight and diagonal) seams are made.

3. Warp and weft wires weave is plain weave or 2/1 twill weave.

4. Maximum width of cloth is 7,5 m, length of seamed cloth is from 9,0 m to 54,0 m.