Single layer synthetic fabrics

Material: polyester monofilament (PET)

polypropylene monofilament (PP)

| Fabric number, type of weave and longitudinal section along warp yarns | Maximum cloth’s width, mm | Nominal yarns diameter, mm |  |  | Nominal size of opening between, mm |  | Air permeability, CFM | Cloth’s thickness, mm | Nominal weight of 1 m2 of cloth, kg |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | warp | weft |  | Warp yarns | Weft yarns |  |  |  |  |  |  |
| Fabrics without heatsetting |  |  |  |  |  |  |  |  |  |  |  |  |
| · · · · · plain weave |  |  |  |  |  |  |  |  |  |  |  |  |
| 2 | 4000 | 0.80 | 0.80 |  | 4.20 | 4.20 | 1558 | 1.460-1.485 | 0.380 |  |  |  |
| 3 | 4000 | 0.80 | 0.80 |  | 2.533 | 2.533 | 1394 | 1.435-1.500 | 0.534 |  |  |  |
| 4 | 3000 | 0.65 | 0.70 |  | 1.85 | 1.118 | 1132 | 1.200-1.245 | 0.539 |  |  |  |
| 5,6 | 4000 | 0.80 | 0.80 |  | 0.986 | 0.986 | 768 | 1.520-1.560 | 0.939 |  |  |  |
| 6 | 6000 | 0.65 | 0.80 |  | 1.017 | 1.018 | 869 | 1.610-1.655 | 0.778 |  |  |  |
| 8 | 7000 | 0.65 | 0.80 |  | 0.600 | 0.866 | 581 | 1.550-1.580 | 0.926 |  |  |  |
| 10 | 6000 | 0.55 | 0.70 |  | 0.450 | 0.728 | 558 | 1.355-1.390 | 0.818 |  |  |  |
| 10 | 5000 | 0.45 | 0.60 |  | 0.550 | 0.650 | 623 | 1.120-1.180 | 0.667 |  |  |  |
| 11 | 6000 | 0.45 | 0.60 |  | 0.459 | 0.511 | 492 | 1.100-1.130 | 0.738 |  |  |  |
| 16 | 5000 | 0.35 | 0.50 |  | 0.275 | 0.553 | 505 | 0.935-0.950 | 0.590 |  |  |  |
| · · · · · | ½ twill weave |  |  |  |  |  |  |  |  |  |  |  |
| 14 | 3000 | 0.27 | 0.27 |  | 0.444 | 0.408 | 918 | 0.560-0.590 | 0.255 |  |  |  |
| Fabrics with heatsetting |  |  |  |  |  |  |  |  |  |  |  |  |
| · · · · · plain weave |  |  |  |  |  |  |  |  |  |  |  |  |
| 6 | 4000 | 0.65 | 080 |  | 1.017 | 1.018 | 804-902 | 1.600-1.670 | 0.778 |  |  |  |
| 7 | 4000 | 0.65 | 0.70 |  | 0.779 | 0.729 |  |  | 0.817 |  |  |  |
| 8 | 6000 | 0.65 | 0.80 |  | 0.600 | 1.200 | 633-722 | 1.33-1.58 | 0.884 |  |  |  |
| 8 | 4000 | 0.65 | 0.80 |  | 0.600 | 0.628 |  | 1.33-1.58 | 0.967 |  |  |  |
| 10 | 6000 | 0.55 | 0.70 |  | 0.450 | 0.838 | 578-607 | 1.150-1.300 | 0.812 |  |  |  |
| 11 | 6000 | 0.45 | 0.60 |  | 0.460 | 0.650 | 433-508 | 0.950-1.000 | 0.652 |  |  |  |
| 12 | 4000 | 0.30 | 0.32 |  | 0.533 | 0.513 | 574 | 0.596-0.605 | 0.285 |  |  |  |
| 16 | 5000 | 0.35 | 0.50 |  | 0.275 | 0.676 | 511-590 | 0.710-0.784 | 0.511 |  |  |  |
| 17,5 | 4000 | 0.27 | 0.27 |  | 0.300 | 0.355 | 1000 | 0,615-0,630 | 0,29 |  |  |  |
| · · · · · 4/1 satin weave |  |  |  |  |  |  |  |  |  |  |  |  |
| 21 | 7000 | 0.27 | 0.32 |  | 0.206 | 0.193 | 524-656 | 0.70-0.78 | 0.443 |  |  |  |
| · · · · · 2/1 twill weave |  |  |  |  |  |  |  |  |  |  |  |  |
| 9 | 4500 | 0.65 | 0.80 |  | 0.461 | 0.628 | 558-623 | 1.42-1.49 | 1.050 |  |  |  |
| 13 | 7000 | 0.65 | 0.80 |  | 0.119 | 2.533 | 787-820 | 1.84-1.89 | 1.025 |  |  |  |
| 13 | 000 | 0,65 | 0.80 |  | 0.119 | 0.867 | 262-328 |  | 1.233 |  |  |  |
| 14 | 2500 | 0.27 | 0.30 |  | 0.444 | 0.414 | 918 | 0.560-0.590 | 0.283 |  |  |  |
| · · · · · 3/1 twill weave |  |  |  |  |  |  |  |  |  |  |  |  |
| 24 | 9000 | 0.25 | 0.30 |  | 0.167 | 0.240 | 394-538 | 0.60-0.67 | 0.406 |  |  |  |
| 24 | 9000 | 0.25 | 0.27 |  | 0.167 | 0.243 | 394-525 | 0.58-0.65 | 0.375 |  |  |  |
| 26 | 9000 | 0.22 | 0.25 |  | 0.165 | 0.263 | 525-656 | 0.56-0.62 | 0.317 |  |  |  |
| 26 | 9000 | 0,22 | 0,27 |  | 0,165 | 0.256 | 492-623 | 0.58-0.60 | 0.334 |  |  |  |
| 28 | 9000 | 0.22 | 0.24 |  | 0.137 | 0.248 | 443-591 | 0.52-0.57 | 0.324 |  |  |  |
| 30 | 9000 | 0.20 | 0.24 |  | 0.133 | 0.225 | 427-558 | 0.48-0.53 | 0.310 |  |  |  |
| 32 | 9000 | 0.20 | 0.24 |  | 0.113 | 0.214 | 443-541 | 0.49-0.51 | 0.328 |  |  |  |
| 32 | 9000 | 0.20 | 0.22 |  | 0.113 | 0.224 | 476-558 | 0.46-0.51 | 0.301 |  |  |  |
| 40 | 9000 | 0.15 | 0.20 |  | 0.100 | 0.177 | 377-459 | 0.36-0.40 | 0.248 |  |  |  |

NOTE:

1. Fabric number indicates nominal number of warp yarns per running centimeter.

2. Fabrics are produced as a seamed (endless) or seamless cloth. In endless cloth the following seams are used:  sewn, loop detachable, spiral or clipper detachable, woven straight and woven diagonal.

3. Fabrics from 15 to 55 m long are treated on tension machine with heatsetting; seam zone on fabrics less than 15 m long undergoes heating on tension machine. Endless fabrics No.No. 21-40 from 15 to 55 m long undergo grinding if agreed upon by the parties.

4. Endless fabrics are delivered with cut and melted edges only; seamless cloths can be delivered with both edges cut; with both edges uncut; with one edge cut and the other edge uncut; if required by the customer edges can be glued from 8 to 30 mm width.

5. Fabric’s cost is calculated according to its size and additional treatment as mentioned: seaming, heatsetting, edge overstitching, edge gluing.

Physical characteristics of synthetic woven fabrics

| Fabric strength, kg/cm | 52 -180 |
| --- | --- |
| Relative elongation of fabric along warp yarns after heatsetting at 10 kg/cm load, % | 0.6 – 0.7 |
| Temperature of polyester emolliating, °C | +230 – (+249) |
| Fabric working temperature, °C - working temperature of fabrics made of polypropylene | (-40) – (+60) from -15°C to +60°C |

Synthetic fabrics made of polyester monofilament

- are resistant to mineral and organic acids,  alkalis (with concentration not more than 10%, pH 9-11) and organic solvents (acetone, benzene, 4-chloride carbon);

- have high resistance to atmospheric exposure, are not dissolved in water, have biochemical resistance, are good electric insulting materials;

- are dissolved in phenols, concentrated sulfuric acid and hydrogen nitrate;

- must not be subject to prolonged exposure of a high temperature steam (above +110°C) because it causes hydrolytic destruction of monofilament and decline in strength;

- synthetic fabrics made of polyester monofilament, containing also polyamide yarns, mustn’t be cleaned with mineral and organic acids as well as chemicals with oxidizing properties (for example, peroxides), because it may lead to polyamide yarns destruction.