| Brass woven wire cloth with square meshes Width of cloth-1000mm. Plain weave. Material-brass wire L-80. Brass woven wire cloth used for filtering element of medical apparatus.. Gauze №; Aperture, mm; Wire diameter, mm; Wire diameter, inch; Mesh; Open area, %; Weight in kgs per 1 sq.m.. 2,2; 2,2; 0,8; 0,032; 8,5; 53,8; 3,1. 4; 4,0; 1,0; 0,039; 5,1; 64; 2,85. Width of cloth - 1000, 1300, 1500 mm. Plain weave. Material-brass wire L-80 Gauze №; Aperture, mm; Wire diameter, mm; Wire diameter, inch; Mesh; Open area, %; Weight in kgs per 1 sq.m. 45; 0,45; 0,20; 0,008; 39,1; 47,9; 0,86. 05; 0,5; 0,25; 0,010; 33,9; 44,4; 1,16. 056; 0,56; 0,25; 0,010; 31,4; 47,8; 1,08. 063; 0,63; 0,30; 0,012; 27,3; 45,9; 1,35. 07; 0,7; 0,30; 0,012; 25,4; 79,0; 1,26. 08; 0,8; 0,30; 0,012; 23,1; 52,9; 1,14. 09; 0,9; 0,40; 0,016; 19,5; 47,9; 1,72. 1; 1; 0,40; 0,016; 18,1; 51,0; 1,60. 1,25; 1,25; 0,40; 0,016; 15,4; 57,4; 1,36. 1,6; 1,6; 0,50; 0,020; 12,1; 58,1; 1,66. 2; 2; 0,50; 0,020; 10,2; 64,0; 1,40. 2,5; 2,5; 0,50; 0,020; 8,5; 69,4; 1,16. |  |
| --- | --- |