| Solid-drawn weldless netting Material- coldly pull sheet of low carbon steel or stainless steel, thickness 0.7-1.2mm, width-1000mm, length- 1500-2500mm. Netting can have another dimension of mesh and different step of list feeding. Solid -drawn netting could be covered by PVC. Designation; Dimension of big diagonal; Dimension of small diagonal; Step of listfeeding, mm. mm; inch; mm; inch. SDWN-15; 15; 0.59; 6.0; 0.24; 1.5. SDWN-20; 20; 0.79; 7.5; 0.30; 1.6. SDWN-25; 25; 0.98; 9.0; 0.35; 2.3. SDWN-30; 30; 1.18; 11.5; 0.45; 2.5. SDWN-40; 40; 1.57; 15.5; 0.61; 3.0. |  |
| --- | --- |