## Special woven wire mesh

Application: in production of wooden fiber boards and wooden shaving boards; on supplementary equipment of pulp-and-paper production; for separating of materials according to particles’ size; for filtering of water, oil, other liquids and solutions in chemical, gas industries, power engineering and other industries.

| Mesh № | Nominal wire diameter of warp and weft, mm | Size of opening between, mm |  | Nominal weight of 1m2 of cloth, kg |
| --- | --- | --- | --- | --- |
|  |  | warp wires | weft wires |  |
| Brass 80/20 |  |  |  |  |
| 36 | 0.12 | 0.158 | 0.158 | 0.732 |
| 34 | 0.12 | 0.174 | 0.174 | 0.693 |
| 32 | 0.12 | 0.193 | 0.193 | 0.652 |
| 30 | 0.12 | 0.213 | 0.213 | 0.613 |
| 28 | 0.12 | 0.237 | 0.237 | 0.572 |
| 26 | 0.14 | 0.245 | 0.245 | 0.724 |
| 24 | 0.14 | 0.277 | 0.277 | 0.669 |
| 22 | 0.16 | 0.294 | 0.294 | 0.803 |
| 22 | 0.22 | 0.235 | 0.235 | 1.517 |
| 20 | 0.16 | 0.340 | 0.340 | 0.732 |
| 20 | 0.22 | 0.280 | 0.280 | 1.383 |
| 18 | 0.16 | 0.396 | 0.396 | 0.654 |
| 16 | 0.20 | 0.425 | 0.425 | 0.911 |
| 16 | 0.25 | 0.375 | 0.375 | 1.345 |
| 14 | 0.25 | 0.464 | 0.464 | 1.251 |
| 12,5 | 0.30 | 0.500 | 0.500 | 1.614 |
| 12 | 0.25 | 0.583 | 0.583 | 1.078 |
| 11 | 0.30 | 0.609 | 0.609 | 1.429 |
| 11 | 0.25 | 0.659 | 0.659 | 0.992 |
| 10 | 0.30 | 0.700 | 0.700 | 1.304 |
| 9 | 0.30 | 0.811 | 0.811 | 1.180 |
| 8 | 0.40 | 0.850 | 0.850 | 1.877 |
| 7.2 | 0.40 | 0.989 | 0.989 | 1.701 |
| 6 | 0.40 | 1.267 | 1.267 | 1.435 |
| 4.8 | 0.50 | 1.583 | 1.583 | 1.829 |
| 4 | 0.50 | 2.00 | 2.00 | 1.553 |
| 3 | 0.50 | 2.833 | 2.833 | 1.208 |
| 7.2/6.4 | 0.50 | 0.889 | 1.063 | 2.521 |
| Tin-phosphor bronze BrOPh 6.5-0.4 |  |  |  |  |
| 21 | 0.23 | 0.246 | 0.246 | 1.627 |
| 12 | 0.25 | 0.583 | 0.583 | 1.107 |
| 11.2 | 0.30 | 0.593 | 0.593 | 1.491 |
| 9 | 0.50 | 0.611 | 0.611 | 3.363 |
| 7.2/6.4 | 0.50 | 0.889 | 1.063 | 2.726 |
| 5.6 | 0.50 | 1.285 | 1.285 | 2.159 |
| 4.8 | 0.50 | 1.583 | 1.583 | 1.876 |
| 4 | 0.50 | 2.000 | 2.000 | 1.593 |
| Stainless steel AISI 304, AISI 316, AISI 321 |  |  |  |  |
| 38.5 | 0.10 | 0.160 | 0.160 | 0.504 |
| 32 | 0.15 | 0.163 | 0.163 | 0.944 |
| 25 | 0.20 | 0.200 | 0.200 | 1.318 |
| 22 | 0.20 | 0.255 | 0.255 | 1.163 |
| 20 | 0.20 | 0.300 | 0.300 | 1.060 |
| 20 | 0.10 | 0.400 | 0.400 | 0.265 |
| 18 | 0.25 | 0.306 | 0.306 | 1.494 |
| 16 | 0.25 | 0.375 | 0.375 | 1.333 |
| 16 | 0.20 | 0.425 | 0.425 | 0.853 |
| 14 | 0.25 | 0.464 | 0.464 | 1.171 |
| 13 | 0.25 | 0.519 | 0.519 | 1.090 |
| 13 | 0.22 | 0.549 | 0.549 | 0.844 |
| 13 | 0.15 | 0.619 | 0.619 | 0.393 |
| 12.5 | 0.25 | 0.550 | 0.550 | 1.272 |
| 12(twill weave ) | 0.40 | 0.433 | 0.433 | 2.068 |
| 11 | 0.25 | 0.659 | 0.659 | 0.929 |
| 11 | 0.30 | 0.609 | 0.609 | 1.337 |
| 10 | 0.25 | 0.750 | 0.750 | 0.840 |
| 10 | 0.40 | 0.600 | 0.600 | 2.170 |
| 9 | 0.35 | 0.761 | 0.761 | 1.498 |
| 9 | 0.30 | 0.811 | 0.811 | 1.094 |
| 9 | 0.25 | 0.861 | 0.861 | 0.760 |
| 8 | 0.40 | 0.850 | 0.850 | 1.740 |
| 7.5 | 0.40 | 0.933 | 0.933 | 1.638 |
| 7.2 | 0.40 | 0.989 | 0.989 | 1.576 |
| 6 | 0.50 | 1.167 | 1.167 | 2.078 |
| 6 | 0.40 | 1.267 | 1.267 | 1.330 |
| 5.6 | 0.50 | 1.285 | 1.285 | 1.951 |
| 5 | 0,50 | 1.500 | 1.500 | 1.759 |
| 4.8 | 0.50 | 1.583 | 1.583 | 1.679 |
| 4.5 | 0.50 | 1.722 | 1.722 | 1.583 |
| 4 | 0.70 | 1.800 | 1.800 | 2.793 |
| 4 | 0.50 | 2.000 | 2.000 | 1.425 |
| 3.3 | 0.50 | 2.530 | 2.530 | 1.204 |
| 3 | 1.00 | 2.333 | 2.333 | 4.434 |
| 3 | 0.50 | 2.833 | 2.833 | 1.108 |
| 2.5 | 1.00 | 3.000 | 3.000 | 3.782 |
| 2 | 1.00 | 4.000 | 4.000 | 2.899 |
| 1.25 | 1.00 | 7.000 | 7.000 | 1.954 |
| 1 | 1.00 | 9.000 | 9.000 | 1.639 |
| 7.2/6.4 | 0.50 | 0.889 | 1.063 | 2.338 |
| Low-carbon steel St 0, St 1, St 2 |  |  |  |  |
| 4.8 | 0.50 | 1.583 | 1.583 | 1.695 |
| 4 | 0.50 | 2.000 | 2.000 | 1.439 |
| 3 | 1.00 | 2.333 | 2.333 | 4.477 |
| 3 | 0.50 | 2.833 | 2.833 | 1.119 |
| 2.5 | 1.00 | 3.000 | 3.000 | 3.800 |
| 2 | 1.00 | 4.000 | 4.000 | 2.913 |
| 1 | 1.00 | 9.000 | 9.000 | 1.647 |
| 7.2/6.4 | 0.50 | 0.889 | 1.063 | 2.486 |

Notes:

1. Mesh number indicates nominal number of warp wires per centimeter.

2. Maximum width of special wire mesh is 4 m, length of mesh with wire diameter up to 0,5mm inclusively is up to 35m, with wire diameter more than 0,5mm – up to 25m.

3. Meshes are made without a seam. If agreed upon by the parties mesh can be produced with a gas soldered diagonal seam, gas soldered straight seam, sewn seam, loop seam.