| Steel woven wire cloth partially riffled - Steel woven wire cloth partially riffled Plain weave. Used for cleaning clay liquids in oil industry, for manganese ore separation, for sifting non-ferrous, constructive and other materials. Width of materials till number 3/6 - 1300mm, number 1.6-4 - 1000-1750mm. Netting can have different dimension of mesh and diameters of wire. Gauze №.; Aperture, mm; Wire diameter; Mesh; Open area, %; Weight in kgs per 1 sq.m.; Material. mm; inch. 07/2,3; 07/2,3; 0,5/0,7; 0,020/0,028; 21,2/8,5; 44,7; 2,261; Stainless steel 12Х18Н10Т. 1/2,3; 1/2,3; 0,6/0,9; 0,024/0,035; 15,9/7,9; 44,9; 2,886. 1/5; 1/5; 0,7/1,0; 0,028/0,039; 14,9/4,2; 49,0; 2,716. 2,5/5; 2,5/5; 0,7/1,0; 0,028/0,039; 7,9/4,2; 65,1; 1,895. 3/6; 3/6; 0,7/1,0; 0,028/0,039; 6,9/3,6; 69,5; 1,831. 1,6; 1,6; 0,9/1,0; 0,035/0,039; 10,2/9,8; 39,4; 4,8; steel 55. 2; 2,0; 1,2/1,3; 0,047/0,051; 7,9/7,7; 37,9; 6,5. 2,6; 2,6; 1,2; 0,047; 6,7; 46,8; 5,2. 3; 3,0; 1,4; 0,055; 5,8; 46,5; 5,1. 3; 3,0; 1,2; 0,47; 6,1; 51,0; 4,5; Low. 4; 4,0; 1,6; 0,063; 4,5; 51,0; 6,0. - Nichrome woven wire cloth partially riffled Plain weave. Width of cloth - 625, 1250, 1875 mm. Material-Nichrome wire Х20Н80, Х15Н60. Gauze No.; Aperture, mm; Wire diameter; Mesh; Open area, %; Weight in kgs per 1 sq.m. mm; inch. 4; 4,0; 1,6; 0,063; 4,5; 51,0; 6,53. 10; 10,0; 3,0; 0,118; 1,95; 59,2; 9,70. 12; 12,0; 3,0; 0,118; 1,69; 64,0; 8,35. 20; 20,0; 3,6; 0,142; 1,08; 71,8; 7,73. 25; 25,0; 3,6; 0,142; 0,89; 76,4; 6,22. |  |
| --- | --- |