| Strand Filtering Woven Wire cloth Strand Filtering Woven Wire Cloth consists of wire strands in warp and weft. Warp strand consists of five wires, weft strand consists of seven wires. Twilled weave. Width of cloth-1000mm. Material-monel НМЖМЦ-28-2,5-1,5. Used for filtering of oil products.. Gauze №; Number of strands per 1 inch; Wire diameter in strand, mm; Wire diameter in strand, inch; Number of strands; Weight in kgs per 1 sq.m.. warp; weft; warp; weft; warp; weft; warp; weft. 140/140; 35,6; 35,6; 0,18; 0,12; 0,007; 0,005; 5; 8; 2,8. |  |
| --- | --- |