Torque netting

|  | Material-heat treated low carbon wire. Mesh size 100 can be produced from galvanized wire. Length of roll is 50 meters or more. Aperture is distance between opposite sides of hexahedron. |
| --- | --- |

| Aperture, mm | Wire diameter |  | Width, mm | Weight in kgs per 1 sq.m. |
| --- | --- | --- | --- | --- |
|  | mm | inch |  |  |
| 25 | 0,6 | 0,024 | 500, 1000, 1500, 2000 | 0,252 |
| 100 | 0,6 | 0,024 | 1000, 1500, 2000, 2500, 3000 | 0,068 |