Twisted woven wire mesh

Application: in pulp-and-paper industry for production of pulp, cardboard, thick wrapping paper, wooden fiber plates; in geology.

| Mesh № | Material |  | Nominal wire diameter, mm |  | Size of opening between, mm |  | Nominal weight of 1 m2 of mesh, kg |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | warp | weft | warp | weft | warp | weft |  |
| 7.2 | Tin-phosphor bronze, BrОPh 6.5 - 0.4 (8.0 – 0.3) | Brass 80/29 | 0.22х7 | 0.45 | 0.729 | 0.883 | 3.037 |
| 7.2 |  | BrОPh 6.5-0.4 | 0.22х7 | 0.45 | 0.729 | 0.883 | 3.057 |
| 7.2 |  | BrОPh 6.5-0.4 | 0.22х7 | 0.18х7 | 0.729 | 0.793 | 3.385 |
| 7.2 |  | polyester | 0.22х7 | 0.70 | 0.729 |  | 2.448 |
| 10 |  | Brass 80/20 | 0.18х7 | 0.40 | 0.460 | 0.780 | 2.762 |
| 10 |  | BrОPh 6.5-0.4 | 0.18х7 | 0.40 | 0.460 | 0.780 | 2.781 |
| 10 |  | BrОPh 6.5-0.4 | 0.18х7 | 0.15х7 | 0.460 | 0.726 | 2.937 |
| 10 |  | polyester | 0.18х7 | 0.70 | 0.460 |  | 2.325 |
| 11 |  | Brass 80/20 | 0.15х7 | 0.37 | 0.459 | 0.630 | 2.333 |
| 11 |  | BrОPh 6.5-0.4 | 0.15х7 | 0.37 | 0.459 | 0.630 | 2.348 |
| 11 |  | BrОPh 6.5-0.4 | 0.15х7 | 0.40 | 0.459 | 0.600 | 2.508 |
| 16 |  | Brass 80/20 | 0.12х7 | 0.27 | 0.265 | 0.471 | 2.005 |
| 10 | Stainless steel AISI 321, AISI 316 |  | 0.18х7 | 0.40 | 0.460 | 0.776 | 2.525 |
| 11 | - « - |  | 0.15х7 | 0.37 | 0.459 | 0.630 | 2.110 |

Note:

- Mesh number indicates nominal number of twisted warp wires per centimeter.

- A twisted warp wire is made of 7 wires by twisting them together.

- In endless twisted meshes made of non-ferrous metals the following seams are used: sewn, woven, loop, gas soldered.

- Meshes are produced up to 7,0 m wide. Length of seamed meshes can be from 9,00m to 54,00 m.