Welded mesh for glass reinforcement and heat insulation

Material-low-carbon steel wire. 
Cross wires of welded mesh for glass reinforcement have double rifle in each mesh.

| Pitch by axles of line and cross wires | Wire diameter |  | Width, mm | Weight in kgs per 1 sq.m. | Length of roll, m |
| --- | --- | --- | --- | --- | --- |
|  | mm | inch |  |  |  |
| 12,5 | 0,50 | 0,02 | 1175 | 0,24 | 100-200 |
| 12,5 | 0,60 | 0,02 | 600, 800, 1000,1600 | 0,352 |  |
| 25,0 | 0,60 | 0,02 | 2000, 2400, 2600 | 0,176 |  |
| 25,0 | 0,80 | 0,03 | 600, 800, 1000, 1600 | 0,312 |  |