| Welded mesh galvanized and ungalvanized. Material- low carbon cold drawing wire with diameter 1.2-4.0 mm of round profile and diameter 3.0-4.0 mm of periodical profile. Breaking load for welding mesh from wire diameter 2.0 mm and more is 295 N (min), and from wire diameter 1.4-1.6mm is 147N (min). Welded mesh can be produced ungalvanized and hot galvanized. Approximate weight of roll is less 500 kgs, length of roll-15-33.3m. Welded mesh can have intermediate width and different dimensions between wire’s axles. Width of roll-350-2000mm Pitch by axles of line and cross wires; Wire diameter; Weight in kgs pre 1 sq.m.. mm; inch. 10/10; 1,4; 0,055; 2,43. 12,5/12,5; 1,4; 0,055; 1,94. 20/20; 1,2; 0,047; 0,9. 25/25; 1,4; 0,055; 0,98. 1,6; 0,063; 1,28. 2,0; 0,079; 2. 25/12,5; 1,4; 0,055; 1,46. 2,0; 0,079; 2,98. 25/50; 2,0; 0,079; 1,5. 50/12,5; 1,2; 0,047; 0,9. 2,0; 0,079; 2,49. 50/25; 2,0; 0,079; 1,5. 50/50; 1,4; 0,055; 0,5. 1,6; 0,063; 0,65. 2,0; 0,079; 1,01. 2,5; 0,098; 1,58. 2,8; 0,110; 1,98. 3,0; 0,118; 2,27. 100/50; 2,0; 0,079; 0,76. 2,5; 0,098; 1,19. 37,5/50; 1,9; 0,075; 1,06. 62,5/50; 1,9; 0,075; 0,82. 2,5; 0,098; 1,42. 50/62,5; 1,9; 0,075; 0,82. 2,5; 0,098; 1,42. 75/50; 1,9; 0,075; 0,75. 2,5; 0,098; 1,31. 2,0; 0,079; 0,84. 75/75; 2,5; 0,098; 1,05. 50/75; 1,9; 0,075; 0,77. 2,5; 0,098; 1,32. 4,0; 0,157; 3,38. 75/62,5; 2,5; 0,098; 1,16. 150/75; 2,8; 0,110; 1. 150/50; 2,8; 0,110; 1,32. 100/100; 4,0; 0,157; 2,07. 3,0; 0,118; 1,16. 150/150; 3,0; 0,118; 0,88. 4,0; 0,157; 1,38. 100/150; 3,0; 0,118; 0,98. 4,0; 0,157; 1,74. 150/100; 3,0; 0,118; 0,96. 4,0; 0,157; 1,71. 200/150; 3,0; 0,118; 0,7. 4,0; 0,157; 1,25. 187,5/200/50; 2,8; 0,11; 1,36. 250/50; 2,5; 0,098; 1,04. 2,8; 0,11; 1,31. |  |
| --- | --- |