Woven wire cloth

Materials for wire cloth are stainless steel wire and low carbon wire.
* (Chemical composition of steel and alloys) 
 Warp – longitudinal wires, weft – wires crossing wire cloth .

Definitions: aperture-a ,      wire diameter-d.

Open area F: share in area of apertures in percent

| F = | a2 | •100% |
| --- | --- | --- |
|  | (a+d)2 |  |

Weaving warp wire and weft wire in perpendicular direction forms Woven Wire Cloth.

Application

- Sifting and separation of granular materials;

- Filtering of liquid solutions, air, gases;

- Sorting of crushed abrasive materials;

- dehydration;

- drying;

- Vacuum or pressure filtration;

- Washing of clay liquids in oil industry;

- Conveyer belts;

- Washing of clay liquids in oil industry for manganese ore separation.

| Chemical composition of steel and alloys ### Chemical composition of steel Grade; Chemical composition, %. С; Si; Mn; P; S; Cr; Ni; Mo; Ti; Al; Cu; Fe. 03Х18Н9Т-ВИ; 0,03; 0,8; 2,0; 0,035; 0,020; 17-19; 8-9,5; -; 5С-0,3; -; -; -. 08Х18Н10; 0,08; 0,8; 2,0; 0,035; 0,020; 17-19; 9-11; -; -; -; -; -. 06Х17Н12М3-ПТ; 0,06; 1; 2,0; 0,035; 0,020; 16-18; 10-13,5; 2-3; 0,2; -; -; -. 03Х17Н12М3-ВИ; 0,03; 1; 2,0; 0,035; 0,020; 16-18; 10-13,5; 2-3; 0,05; -; -; -. 03Х18Н12-ВИ; 0,03; 0,4; 0,4; 0,030; 0,020; 17-19; 11,5-13; -; 0,01; -; -; -. 02Х19Н11-ВИ; 0,03; 1; 2,0; 0,035; 0,020; 18-20; 10-12; -; 0,05; -; -; -. 04Х19Н9; 0,06; 0,5-1; 1,0-2,0; 0,025; 0,018; 18-20; 8-10; -; -; -; -; -. 06Х18Н10-ПТ; 0,06; 1; 2,0; 0,035; 0,020; 17-18; 8,5-11; -; 0,20; -; -; -. 12Х18Н9Т; 0,12; 0,8; 2,0; 0,035; 0,020; 17-18; 8-9,5; -; 5С-0,8; -; -; -. 12Х18Н10Т; 0,12; 0,8; 2,0; 0,035; 0,020; 17-18; 9-11; -; 5С-0,8; -; -; -. 12Х18Н9; 0,12; 0,8; 2,0; 0,035; 0,020; 17-18; 8-10; -; -; -; -; -. Св-08; 0,10; 0,03; 0,35-0,6; 0,040; 0,040; 0,15; 0,30; -; -; 0,01; -; -. Св-08А; 0,10; 0,03; 0,35-0,6; 0,030; 0,030; 0,12; 0,25; -; -; 0,01; -; -. Ст.1КП; 0,06-0,12; 0,05; 0,25-0,5; 0,040; 0,050; 0,30; 0,30; -; -; -; -; -. Ст.3ПС; 0,14-0,22; 0,05-0,15; 0,4-0,65; 0,040; 0,050; 0,30; 0,30; -; -; -; -; -. Ст.55; 0,52-0,60; 0,17-0,37; 0,5-0,8; 0,035; 0,040; 0,25; 0,30; -; -; -; 0,3; -. Х15Н60; 0,15; 0,8-1,5; 1,5; 0,030; 0,020; 15-18; 55-61; -; 0,3; 0,3; -; others. Х20Н80; 0,10; 09,1,5; 0,7; 0,030; 0,020; 20-23; others; -; 0,3; 0,2; -; 1,5. ### Chemical composition of alloys. Alloy; Gradeа; Chemical composition, %. Main elements; Impurity elements. Cu; Zn; Pb; Fe; Sb; Bi; P; Total. Brass; Л80; 79-81; others; 0,03; 0,1; 0,005; 0,002; 0,01; 0,3. Alloy; Grade; Chemical composition, %. Main elements; Impurity elements. Al; Fe; Mn; Zn; Ni + Co; Cu; Ti; Pb; Si; Mg. Monel; НМЖМц 28-2,5-1,5; -; 2-3; 1.2-1.8; -; others; 27-29; -; 0,3; 0,05; 0,10. |  |
| --- | --- |